# Spectrum Distributors

415 Umgeni Rd, Durban

T 031-309 6404

www.artjunction.co.za

art24@mweb.co.za

# PROCAT, PROLON & POLYFLEX INKS for NYLON

## PRODUCT INFORMATION

These series of inks have been developed for printing directly onto the wide variety of nylon materials that are used for applications like umbrellas, flags, travel bags and sports outerwear.

Once thoroughly dry (24 hours) these inks show excellent adhesion, scuff resistance and water resistance.

## APPLICATION INFORMATION

Substrate:	In this regard some initial testing may be required.

PROCAT, a two pack system, appears most suited for waterproofed nylons a used for umbrellas and flags.

POLYFLEX is recommended for very coarsely woven materials.

PROLON is more flexible ink than POLYFLEX and is suited for most materials.

Drying:	By solvent evaporation. Air-dry in 20 – 40 minutes. May be jet dried.

Stencils:	Solvent resistant direct emulsion, photographic and hand-cut water-soluble stencils are suitable.

Coverage:	25 – 40 sq. m. per kilo (90 – 120T mesh). Coarser mesh will be needed for dark or coarsely woven materials

Thinners:	D564 S069	PROCAT / PROLON / POLYFLEX THINNERS

D564 S004	UNIVERSAL RETARDER

N660 S344	SCREENWASH

Catalyst:	D590 A104	Use 1 part catalyst / 2 parts PROCAT Ink

CAUTION:	Please proof this ink, reduced to the consistency you wish to adopt, on a sample of the ACTUAL SUBSTRATE you will be printing BEFORE starting a production run. Give the proof 24 hours to dry out then check for: Abrasion resistance, adhesion, print appearance and correctness of colour. The adequacy of this ink in these properties cannot be fully established on laboratory equipment on a small scale. This product is manufactured under laboratory supervision from the finest raw materials and we feel it will perform exactly as represented. However, as we have no control over the use or application thereof, we make no warranties, expressed or implied. Keep away from heat and open flame. Use with adequate ventilation. Avoid prolonged or repeated contact with skin. Avoid prolonged breathing of vapour or spray mist. Keep container closed when not in use.

DATE LAST AMEMDED:	5/08/2002